Types of Stone Typically Used in Monuments:

Limestone

Marble

Granite

Sandstone

Types of Damage Often Incurred:

Mower/Weed-eater Damage

Vandalism Damage (graffiti, purposeful breakage)

Salt Damage (de-icing salts, weed/grass killers, pesticides and improper detergents)

Bleach Damage

Acid Rain Damage

“Rubbing” Damage

Cleaning Monuments:

Pre-soak monument

Clean Water

Light Brushing (soft bristled brushes only)

Approved Salt-Free/Bleach-Free Cleaners (D2-available from Cathedral Stone)

RINSE, RINSE, RINSE

NEVER BLEACH, SHAVING CREAM, HOUSEHOLD CLEANERS

Reading Worn Monuments:

Clean Water Misting

Light Brushing (soft-bristled brushes only)

Mirrors

Foil (pushed onto surface by hand or sponge)

Checking the Condition of Monuments:

Visual Check

Light Sounding (tapping) to check for non-visible cracks

Repairing/ Preserving Damaged Monuments:

Turn Monument Face Down

Fallen Monuments- lift by hand or with hoist back into place, reattach using sacrificial (lime putty) mortar

Socket and Die- Remount in original or new socket using sacrificial mortar

Simple Breaks- stainless steel pins/epoxies

Compound Breaks- Remount on base with stainless pins/epoxies (if sound)

Create new angled base for unsound monuments

If in doubt, find a stone conservator.

Proper Repair Materials

Lime Putty Mortars

2 part Epoxies

Restoration Mortars (Jahn, U.S. Heritage)

D2 Cleaner

Clean Water

NEVER CONCRETE OR ANYTHING CONTAINING PORTLAND CEMENT